# Shield Beads and Round Cable Cores – General

# (PN Product Classes that could apply:  26)

# Refer to the most current revision of the Fair-Rite Products document Visual Inspection – Definitions & General Criteria for irregularity definitions.

Figure 1

# Limits for Chips by Part Size

  - The largest dimension of any chip may never exceed the general maximum set in Visual Inspection – Definitions & General Criteria.

| Core Size | Surf- ace | Max. Size Allowed | Max Qty |
| --- | --- | --- | --- |
| Nominal OD of Less than 0.125in (3.2mm) | A, B | No limit. No broken parts are allowed | N/A |
| Nominal OD of 0.125in (3.2mm) to 0.25in (6.3mm) | A | No limit | N/A |
|  | B | Less than 33.3% (1/3) of the Bead length | 1 |
| Nominal OD greater than 0.25 (6.3mm) to 0.5in (12.7mm) | A | No limit | 3 on each surface, 5 total |
|  | B | Less than 25% (1/4) of the Bead length or 50% (1/2) of the wall thickness, whichever is smaller |  |
| Nominal OD greater than 0.5in (12.7mm) | A | Less than 50% (1/2) of the wall thickness to max of 5 mm | 3 on each surface, 5 total |
|  | B | Less than 25% (1/4) of the Bead length to a max equiv. area of 5 mm x 7 mm; less than max depth of 0.25 mm |  |

- Limits for Cracks

| Crack Type | Max. Size Allowed | Max Qty |
| --- | --- | --- |
| Radiating / Lengthwise | Less than 20% (1/5) of the Wall Thickness | 1 |
| Parallel to Circumference | 33.3% (1/3) of circumference – must be unopened | 1 |

Figure 2

- Limits for Pullout, Bumps, Pits, etc.

| Type | Max. Size Allowed | Max Qty |
| --- | --- | --- |
| Crazing | No limit | N/A |
| Pits | See chip spec. | See chip spec. |
| Bumps | Small to Moderate Bumps that do not interfere with part fit or function are allowed | Unlimited |
| Ragged Edges | Ragged Edges, as defined in Fair-Rite document Visual Inspection – Definitions & General Criteria, are allowed. | Entire length of relevant edge(s) |
| Pullout | 0.003in (0.076mm) deep | Cumulative area of Pullout must be less than 25% (1/4) of the relevant surface area |
| Sticking | No limit | N/A |

- Limits for Flash

| Core ID Size | Max. Size Allowed |
| --- | --- |
| Less than or equal to 0.12in (3mm) | Flash is allowed. However, flash can never interfere with part size. |
| Greater than 0.12in (3mm) | Flash is allowed unless the part is burnished. If the part is burnished, no flash is allowed. Flash can never interfere with part size. |

Associated Documents:

  - Fair-Rite Products: Visual Inspection – Definitions & General Criteria

- Revision History:

| Revision Number | Reason for Change | Revision Date |
| --- | --- | --- |
| 1 | Section 8.0 revised | 4/1/98 |
| 2 | Complete Revision | 10/29/2007 |
| 3 | Revised Section 1.1 | 10/25/10 |
| 4 | Revised Section 1.1 | 8/12/11 |
| 5 | Revised Title | 12/22/23 |

References:

International Electrotechnical Commission (IEC) International Standard 60424-1: Ferrite Cores – Guide on the Limits of Surface Irregularities Part 1: General specification   (First Edition 1999-05)

International Electrotechnical Commission (IEC) International Standard 60424-4: Ferrite Cores – Guide on the Limits of Surface Irregularities Part 4: Ring-cores   (First Edition 2001-02)