0.0	Slugs – Generic  (PN Product Classes that could apply:  30, 40)

1.0	Chips:

1.1	Chips on Surface A which are longer or wider than 1/5 of the diameter of the 	part are unacceptable.

1.2	Chips on Surface B which are longer than 1/10 of the length of the part, or are 	wider than 1/5 of the diameter of the part, are unacceptable.

1.3	Parts with more than two chips are unacceptable.

2.0	Cracks:

2.1	Cracks are unacceptable.

3.0	Ragged Edges:

3.1	Ragged edges which penetrate less than .040 inches into the part are acceptable.

4.0	Pits:

4.1	Pits with diameters less than .050 inches are acceptable.

5.0	Stains and Discolorations:

5.1	Stains and discolorations which do not affect the performance of the part are 	acceptable.

6.0	Pullout:

6.1	For slugs which are less than 2 inches in length, pullout which extends further 	than .003 inches into the part is unacceptable.

6.2	For slugs which are greater than or equal to 2 inches in length, pullout which 	extends further than .005 inches into the part is unacceptable.

6.3	For slugs with inner diameters, pullout which interferes with the inner diameter is 	unacceptable.

6.4	Because of the epoxy coating process, pullout on slugs is not particularly 	problematic.  Questionable parts should be referred to a QC Inspector.

7.0	Revision History:

| Revision Number | Reason for Change | Revision Date |
| --- | --- | --- |
| 1 | Revised Title | 12/22/23 |