0.0 Surface Mount Beads – Generic  (PN Product Classes that could apply:  27)

Figure:1

Figure 2

Figure 3

1.0	Surface Mount Beads – Generic

# 1.1	Limits for Irregularities:

| Type | Location | Max. Size Allowed | Max Count Allowed |
| --- | --- | --- | --- |
| Chips | A | 25% (1/4) of the smaller of length and width of surface | 3 on each surface, 5 total |
| Chips | B & C | 25% (1/4) of the smaller of length and width | 3 on each surface, 5 total |
| Bumps | All surfaces | Small to moderate bumps that do not interfere with dimensions are allowed | Unlimited |
| Pits | All surfaces | 1mm max | 3 on each surface, 5 total |
| Cracks (applies only to figure 2 type designs, all others no cracks allowed | A | 2mm, must be unopened (see figure 3). Open cracks, cracks which weaken the part, or worsen after thermal shock (SOP ELC-27) are not allowed. See engineering for clarification if needed. | 1 |
| Cracks (applies only to figure 2 type designs, all others no cracks allowed | B & C | 2mm adjacent edge to surface A, anywhere else on surface is unacceptable. | 1 |
| Crazing | All surfaces | No limit | N/A |
| Sticking | All Surfaces | No limit | N/A |

Limits for Irregularities (continued):

| Defect Type | Location | Max. Size Allowed | Max Count Allowed |
| --- | --- | --- | --- |
| Pullout | All surfaces | 0.003in (0.076mm) deep | Cumulative area of Pullout must be less than 30% (1/4) of the relevant surface area. |
| Ragged Edges | All edges | Width as defined in Defect Definitions | Entire Edge surfaces |
| Sharp Edges | All edges | N/A | Sharp edges not allowed on burnished cores |
| Stains and discolorations | All edges | N/A | Stains and discolorations which do not affect the performance of the part are acceptable. |

2.0	Associated Documents:

2.1 Fair-Rite Products: Visual Inspection – Definitions & General Criteria

Revision History:

| Revision Number | Reason for Change | Revision Date |
| --- | --- | --- |
| 1 | Revised Section 4.1 | 12/5/2001 |
| 2 | Revised Complete VIC | 7/30/13 |
| 3 | Revised section 1.1 –Chips | 10/20/23 |
| 4 | Revised Title | 12/22/23 |