# Tack Bobbins – General  (PN Product Classes that could apply:  71)

  - Refer to the most current revision of the Fair-Rite Products document Visual Inspection – Definitions & General Criteria for irregularity definitions.

# Tack Bobbins

Figure 1

Figure 2 (particle separation)

# Limits for Irregularities:

| Type | Location | Max. Size Allowed | Max Count Allowed |
| --- | --- | --- | --- |
| Chips | Post top & wall | Longer or wider than 1/2 the post OD for post OD<.250”, 1/3 the post OD for OD>.250” are unacceptable. | 2 on each surface, 3 total |
|  | Surface A, B, & between A & B | Longer or wider than 1/3 of the diameter of the post are unacceptable. | 2 on each surface, 3 total |
| Cracks | Surface A, B | Cracks which radiate more than 1/4 of the way from the post (or the centre of the part) to the edge of the part are unacceptable. | 2 total |
|  | Interface between post and flange | Unopened cracks in this area are acceptable. | NA |
|  | Between surface A & B | Cracks which extend more than 1/2 of the way around the circumference of the part are unacceptable | 2 total |
| Particle Separation | Flange (Figure 2) | No limit On tack bobbins this is typically found in the center of the backwall(flange) on the bottom of the part due to an inherent lower density in this area. Looks like a separation of particles. | N/A |
| Ragged Edges | All surfaces | 1/5 distance between center post and outer edge of flange(See Figure 1) | ¼ circumference |
| Pits, Bumps | All | .020” in diameter and do not interfere with part size. | 3 total |
| Stains, Discolorations | All | Stains and discolorations which do not affect the performance of the part are acceptable. | Unlimited |
| Crazing | All surfaces | No limit. | N/A |
| Flash | All surfaces | Flash is allowed unless the part is burnished. If the part is burnished, no flash is allowed. Flash can never interfere with part size. | N/A |
| Pullout | All Surfaces | For tack bobbins which are less than ½ of an inch in diameter, pullout which extends further than .002 inches into the part is unacceptable. For tack bobbins which are greater than or equal to 1/2 inch in diameter, pullout which extends further than .004 inches into the part is unacceptable. | ½ area of any surface |

- Associated Documents:

  - Fair-Rite Products: Visual Inspection – Definitions & General Criteria

- Revisions:

| Revision Number | Reason for Change | Revision Date |
| --- | --- | --- |
| 1 | Revised the complete VIC | 3/21/11 |
| 2 | Revised Title | 12/22/23 |

References:

International Electrotechnical Commission (IEC) International Standard 60424-1: Ferrite Cores – Guide on the Limits of Surface Irregularities Part 1: General specification   (First Edition 1999-05)