# Toroids – General  (PN Product Classes that could apply:  59)

  - Refer to the most current revision of the Fair-Rite Products document Visual Inspection – Definitions & General Criteria for irregularity definitions.

# Toroids

Figure 1

Figure 2

# Limits for Irregularities - All Toroid Core Types:

| Type | Location | Max. Size Allowed | Max Count Allowed |
| --- | --- | --- | --- |
| Chips | All surfaces | 25% (1/4) of Wall Thickness to a max equiv. area of 5 mm x 7 mm; less than max depth of 0.25 mm | 3 on each surface, 5 total |
| Bumps | All surfaces | Small to moderate Bumps that do not interfere with part fit or function are allowed | Unlimited |
| Pits | All surfaces | 25% (1/4) of Wall Thickness to a maximum of 0.078in (2mm) | 3 on each surface, 5 total |
| Cracks | Radiating | Less than 20% (1/5) of the Wall Thickness | 1 |
|  | Parallel to the circumference | Cumulative length equal to 33.3% (1/3) of the relative core circumference. Open cracks, or cracks which weaken the part are not allowed. Refer to figure 2 for an example of an unacceptable open crack. See engineering for clarification if needed. | Unlimited up to cumulative length allowance |
| Crazing | All surfaces | No limit | N/A |
| Sticking | All Surfaces | No limit | N/A |

Limits for Irregularities Based on Toroid Core Size

| Defect Type | Core Size | Location | Max. Size Allowed | Max Count Allowed |
| --- | --- | --- | --- | --- |
| Pullout | Nominal OD less than 0.5in (12.7mm) | All surfaces | 0.003in (0.076mm) deep | Cumulative area of Pullout must be less than 25% (1/4) of the relevant surface area. |
|  | Nominal OD equal to or greater than 0.5in (12.7mm) |  | 0.005in (0.127mm) deep |  |

  - Limits for Irregularities Based on Burnishing and Coating

| Defect Type | Core Treatment | Location | Max. Size Allowed | Max Count Allowed | Notes |
| --- | --- | --- | --- | --- | --- |
| Partial Coating | Coated Toroids | All surfaces | None | None | All surfaces must be fully coated. Coating must be uniform and fully adhered. |
| Ragged Edges | Burnished and Un-burnished Cores | All edges | Width as defined in Defect Definitions | Entire Edge surfaces |  |
| Sharp Edges | Un-burnished Cores | All edges | N/A | N/A | Sharp edges allowed on unburnished cores only |
|  | Burnished Cores |  | None | None | Sharp edges not allowed on burnished cores |

- Associated Documents:

  - Fair-Rite Products: Visual Inspection – Definitions & General Criteria

- Revisions:

| Revision Number | Reason for Change | Revision Date |
| --- | --- | --- |
| 1 | Tightened specs in 1.2 and 2.3 | 4/1/98 |
| 2 | Revised 1.4. | 8/18/98 |
| 3 | Complete revision | 10/29/2007 |
| 4 | Revised section 1.3 | 4/25/11 |
| 5 | Revised section 1 and 1.1 added figure 2 | 8/12/11 |
| 6 | Revised Title | 12/22/23 |

References:

International Electrotechnical Commission (IEC) International Standard 60424-1: Ferrite Cores – Guide on the Limits of Surface Irregularities Part 1: General specification   (First Edition 1999-05)

International Electrotechnical Commission (IEC) International Standard 60424-4: Ferrite Cores – Guide on the Limits of Surface Irregularities Part 4: Ring-cores   (First Edition 2001-02)