- Multihole Wound Bead – Generic

(PN Product Classes that could apply:  26, 29)

1.0	Chips:

1.1	Surface chips extending from the holes on Surface A which are longer or wider 	than 1/4 of the diameter of the part are unacceptable.

1.2	Chips on Surface B which are longer or wider than 1/4 of the length (C 	dimension) of the part are unacceptable.

1.3	Parts with more than two chips are unacceptable.

2.0	Cracks:

2.1	Spider cracks are unacceptable.

2.2	Small cracks between the holes which do not affect the performance of the part 	are acceptable.

2.3	Radial cracks which are less than .050 inches deep and less than .125 inches long 	and which do not affect the performance of the part are acceptable.

3.0	Ragged Edges:

3.1	Ragged edges which penetrate more than .015 inches into the part are 	unacceptable.

3.2	Sharp edges are unacceptable.

4.0	Pits and Bumps:

4.1	Pits with diameter greater than .020 inches are unacceptable.

5.0	Stains and Discolorations:

5.1	Stains and discolorations which do not affect the performance of the part are 	acceptable.

6.0	Wire:

6.1	Wire shavings on assembled beads are unacceptable.

7.0	Pullout:

7.1	Pullout which interferes with the holes in Surface A is unacceptable.

8.0	Revision History:

| Revision Number | Reason for Change | Revision Date |
| --- | --- | --- |
| 1 | Revised Title | 12/22/23 |