# Basket Cores – Generic  (PN Product Classes that could apply:  05)

1.0     Chips:

1.1      Parts with more than three (3) chips are unacceptable.

1.2      Parts with more than two (2) chips on any one (1) surface are unacceptable

1.3      Chips on the rim which are either longer or wider than 1/2 of the wall thickness are   unacceptable.

1.4      Chips on the Corners which are longer than 1/3 of the overall height of the core are unacceptable.

1.5      Chips on the Back wall cannot exceed the thickness of the Wall

1.6      Chips on the Saddle are unacceptable

2.0      Cracks:

2.1      Parts with more than three (3) cracks are unacceptable.

2.2      Cracks on the Back wall are unacceptable.

2.3      More than two (2) cracks on any one (1) surface are unacceptable.

2.4      The Length of any Crack cannot exceed Twice the wall thickness.

2.5      Cracks on the Saddle are unacceptable.

2.6      A single continuous crack cannot extend into two (2) surfaces.

3.0      Ragged Edges:

3.1      Ragged edges that penetrate more than 1/4 into the thickness of the part are   unacceptable.

3.2      Ragged edges that extend around more than 1/2 of any one (1) side are

unacceptable.

3.3      Sharp edges are unacceptable.

4.0     Pullouts:

4.1     Pull-Outs on any one (1) surface cannot exceed 25% of the surface area.

4.2     Pull-Outs cannot exceed .005 inches in depth.

5.0     Pits and Bumps:

5.1     Pits /Bumps with diameters greater than .025 inches are unacceptable and are to be

considered chips.

5.2     Parts with more than three pits / bumps are unacceptable.

  - Cleanliness:

  - Stains and discolorations that do not affect the performance of the part are

acceptable.

  - All surfaces of the core should be free of loose particles or any other matter.

7.0      Note:  Cores to be inspected under good light conditions, but without any visual  magnification.

8.0    Revision History:

| Revision Number | Reason for Change | Revision Date |
| --- | --- | --- |
| 1 | Revised Title | 12/22/23 |