# Pot Cores – General  (PN Product Classes that could apply:  55-58)

# Refer to the most current revision of the Fair-Rite Products document Visual Inspection – Definitions & General Criteria for irregularity definitions.

Figure 1

Total count limit for chips on any Pot Core is six (6) maximum, with no more than four (4) on any one (1) surface unless otherwise noted.

### Limits for Mating Surface Irregularities – figure 1

| Type | Location | Maximum Size Allowed | Max Qty |
| --- | --- | --- | --- |
| Chips | Outer Wall | Maximum size of a mating surface chip cannot be greater than 50% (½) the Outer Wall Thickness. | 2 |
|  | Center Post* (ungapped) |  |  |
| Cracks | Outer Wall | Cumulative length less than 50% (½) of Outer Wall thickness | -- |
|  | Center Post* (ungapped, with Hole) | Cumulative length less than 100% of Center Post Wall thickness. Single crack length less than 50% (½) | -- |
|  | Center Post* (ungapped, No Hole) | Cumulative length less than 25% (¼) of Center Post diameter. | -- |
| Ragged Edges | Mating Surface Edges and ungapped Center Post* | Cumulative length less than 25% (¼) of the length of the relevant circumference. | -- |

* See section 3 – Limits for Coil Space and Non-Mating Surface Center Post Irregularities for gapped Center Post and Non-Mating Surface Center Post irregularities.

Figure 2

- Limits for Coil Space and Non-Mating Surface Center Post Irregularities – figure 2

| Type | Location | Maximum Size Allowed | Max Qty |
| --- | --- | --- | --- |
| Chips | Center Post, Non-Mating Surface | 25% (¼) of Center Post Height (CH) | 3 |
|  | Center Post* (gapped, with hole) | Maximum size of a top surface chip cannot be greater than 50% (½) the Center Post wall thickness. | 2 |
|  | Center Post* (gapped, no hole) | Maximum size of a top surface chip cannot be greater than 25% (¼) the Center Post diameter. |  |
| Cracks | Center Post Base | Cumulative length less than 25% (¼) of the Center Post circumference - must be unopened. | -- |
|  | Outer Wall Base | Cumulative length less than 12% (1/8) of the Center Post circumference - must be unopened. | -- |
| Ragged Edges | Center Post* (gapped) | 100% of Center Post inner or outer Circumference | -- |
| Pullout | Bottom of Coil Space | Less than 0.003in (0.076mm) deep | Less than 25% (¼) of the bottom area |
| Sticking |  | Less than 0.001in (0.025mm) deep | 100% of bottom area |

* See section 2 - Allowable Mating Surface Irregularities for ungapped Center Post and Center Post Mating Surface criteria

Figure 3

###### Limits for Wire Slot and Wire Way Area Irregularities– figure 3

| Type | Location | Maximum Size Allowed | Max Qty | Notes |
| --- | --- | --- | --- | --- |
| Chips | Wire Way | 50% (½) of Core Height | 2 | Rule applies to chips beginning at the mating surface and down or beginning at the back surface up |
|  | Wire Slot Mating Surface Areas | Width and length may be 100% of Outer Wall Thickness in size | 4 |  |
| Cracks | Wire Way | Cumulative length less than 50% (½) of the Wire Way Depth | -- | Applies to each Wire Way. Cracks must not be open |
|  | Wire Slot | Less than 100% of the Outer Wall Thickness | 4 per slot edge |  |
| Flash | Wire Slot | 0 | 0 | Flash not allowed in Wire Slot area. |

Figure 4

- Limits for Exterior Wall Surface Irregularities – figure 4

| Type | Location | Maximum Size Allowed | Max Qty |
| --- | --- | --- | --- |
| Chips | Sidewall | Less than 50% (½) of Core Height | 4 |
| Cracks | Sidewall (Horizontal) | None allowed | 0 |
|  | Sidewall (Vertical) | Less than 25% (¼) of Core Height | 2 |

Figure 5

- Limits for Back Surface Irregularities – figure 5

| Type | Location | Maximum Size Allowed | Max Qty | Notes |
| --- | --- | --- | --- | --- |
| Chips | Back Surface | Less than 50% (½) of the Core Height | 4 |  |
|  | Back Surface Wire Slot | 100% Outer Wall thickness | 4 |  |
| Cracks | Parallel to Wire Way | 100% Length of Wire Slot | 2 | Surface Cracks only: open or through cracks, visible on both sides, not allowed |
|  | Radiating from Center Hole | Cumulative length less than 10% (1/10) of core OD | -- |  |
|  | Radiating from Edge | 25% (¼) of core OD | 1 |  |
|  | Radiating from Wire Way | Cumulative length in each Wire Way less than 50% (½) of the Wire Way Depth | -- | Must not be open |
| Ragged Edges | Outer or inner Edge | 20% (1/5) of the relative circumference | 1 |  |

- Associated Documents:

  - Fair-Rite Products: Visual Inspection – Definitions & General Criteria

##### Revision History

| Revision Number | Reason for Change | Revision Date |
| --- | --- | --- |
| 1 | Revised Title | 12/22/23 |

References:

International Electrotechnical Commission (IEC) International Standard 60424-1: Ferrite Cores – Guide on the Limits of Surface Irregularities Part 1: General specification   (First Edition 1999-05)

International Electrotechnical Commission (IEC) International Standard 60424-2: Ferrite Cores – Guide on the Limits of Surface Irregularities Part 2: RM-cores   (First Edition 1997-10)

Magnetic Materials Producers Association (MMPA) MMPA Standard PC 110: Standard Specifications for Ferrite Pot Cores  (Revised January, 1984)