# U, E, I Cores – General  (PN Product Classes that could apply:  90, 92, 93, 94)

  - Refer to the most current revision of the Fair-Rite Products document Visual Inspection – Definitions & General Criteria for irregularity definitions.

# U, E, I Cores

# Limits for Irregularities - All U, E, I Core Types:

| Type | Location | Max. Size Allowed (reference dimension is defined as smallest dimension of surface under consideration) | Max Count Allowed |
| --- | --- | --- | --- |
| Chips | Non-mating surfaces | Largest dimension equal to 1/2 of the reference dimension to a max equiv. area of 5 mm x 7 mm | U Core- 7, E Core- 5, I Core- 2 |
| Chips | Mating surfaces | Largest dimension equal to 1/3 of the reference dimension to a max equiv. area of 5 mm x 7 mm | U Core- 2, E Core- 3, I Core- 2 |
| Cracks | Non-mating surfaces | Largest dimension equal to 1/4 of the reference dimension (cracks parallel to the flux path are acceptable but are not to exceed a count of 5) | U Core- 2, E Core- 2, I Core- 2 |
| Cracks | Mating surfaces | Sum of total cracks for each surface is equal to 1/2 the reference dimension | N/A |
| Pits, Voids | All surfaces | Considered as chips | See above |
| Flash | All surfaces | No limit. Cannot result in nonconforming dimension | N/A |
| Pullout | All Surfaces | 0.005in (0.127mm) deep | Cumulative area of Pullout must be less than 25% (1/4) of relevant surface area |

  - All mating surfaces shall be free of dirt or any other foreign matter.

  - Any stain, discoloration or surface crazing that does not interfere mechanically or electrically is allowed.

- Associated Documents:

  - Fair-Rite Products: Visual Inspection – Definitions & General Criteria

- Revisions:

| Revision Number | Reason for Change | Revision Date |
| --- | --- | --- |
| 1 | Created document based on VIC_U, E, I Cores (excerpt from MMPA defined criteria) | 11/7/14 |
| 2 | Revised section 1.1 | 12/16/15 |
| 3 | Revised Title | 12/22/23 |

References:

MMPA STANDARD NO. UEI 310 (Revised September 1988)