0.0	Multiaperture Cores – Generic (PN Product Classes that could apply:  28)

1.0	Chips:

1.1	Parts with more than three chips are unacceptable.

1.2	Chips that penetrate the holes on surface A are unacceptable.

1.3	For parts with chamfered holes, chips on the chamfer which do not extend into the 	hole and are not visible from Surface B or Surface C are acceptable.

2.0	Cracks:

2.1	Cracks radiating from the holes in surface A are unacceptable.

2.2	Cracks which run up and down the C dimension on Surface B or Surface C are 	unacceptable.

2.3	Surface crazing is acceptable.

3.0	Ragged Edges:

3.1	Ragged edges that penetrate more than 1/10 of the width of the part are 	unacceptable.

3.2	Sharp edges are unacceptable.

4.0	Pits and Bumps:

4.1	Refer to chip specifications.

5.0	Stains and Discoloration:

5.1	Stains and discoloration that do not affect the performance of the part are 	acceptable.

6.0	Pullout:

6.1	Total area shall not exceed 25% of surface A.

6.2	Shall not exceed a depth of 0.003 inches.

6.3	Shall not penetrate the apertures (holes) in surface A.

7.0	Questionable parts should be referred to a QC Inspector.

8.0	Revision History:

| Revision Number | Reason for Change | Revision Date |
| --- | --- | --- |
| 1 | deleted sections 1.3 to 1.5, renumbered 1.6 now 1.3 , revised section 6.1 added sections 6.2,6.3 | 10/1/99 |
| 2 | Revised Title | 12/22/23 |