(PN Product Classes that could apply:  43, 50, 51)

Figure 1

Pull a random sample of parts for visual inspection based on a c=0 sampling plan with an AQL of 0.25. See chart listed in SOP I&T-01. All inspections listed below shall be done at 10X magnification unless otherwise specified.

# 1.0 Limits for Irregularities:

| Type | Location | Max. Size Allowed | Max Count Allowed |
| --- | --- | --- | --- |
| Chips | Rim including any notches | 10% of rim area | No limit on number, total coverage <10% |
|  | Wall & backwall | 10% of surface | No limit on number, total coverage <10% |
| Cracks | Interface between wall & backwall | Unopened cracks in this area are acceptable. | NA |
|  | Backwall | Longer than 1/4 of the distance from the inner diameter(hole) or part center to the inner wall are unacceptable. | 2 total |
|  | Parallel to the circumference | Cumulative length equal to 33.3% (1/3) of the relative core circumference. Open cracks, or cracks which weaken the part are not allowed. Refer to figure 1 for an example of an unacceptable open crack. See engineering for clarification if needed. | Unlimited up to cumulative length allowance |
| Particle Separation | Backwall | No limit This is typically found in the center of the backwall on the bottom of the part due to an inherent lower density in this area. Looks like a separation of particles. | N/A |
| Ragged Edges | All surfaces | 30% of rim and backwall surfaces. | No limit on number, total coverage <30% of perimeter |
| Pits, Bumps | All | Bumps not to interfere with dimensions, pits no larger than 5% of surface area. | 3 total |
| Stains, Discolorations | All | Stains and discolorations which do not affect the performance of the part are acceptable. | No limit on number |
| Crazing | All surfaces | N/A | N/A |
| Flash | All surfaces, OD or smaller overall dimension less than .250” | .002” max height over full perimeter, with a max thickness of .002” | N/A |
|  | All surfaces, OD or smaller overall dimension greater than .250” | .003” max height over full perimeter, with a max thickness of .003” | N/A |
| Pullout | All Surfaces with exception of inside of backwall(floor of cup) | Pullout which extends further than .003 inches into the part is unacceptable. | No limit, 25% of each area. |
|  | Inside of backwall (floor of cup) | Pullout which extends further than .002 inches into the part is unacceptable | No limit |

- Revision History:

| Revision Number | Reason for Change | Revision Date |
| --- | --- | --- |
| 1 | Revised Complete VIC | 11/10/11 |
| 2 | Revised section 1.0 | 9/24/13 |
| 3 | Revised Title | 12/22/23 |