0.0	      Discs – Generic  (PN Product Classes that could apply:  50-53)

1.0	Chips

| Core Size | Surf- ace | Max. Size Allowed | Max Qty |
| --- | --- | --- | --- |
| Figure 1 Nominal OD of less than 1.00in. (25.4mm) | A | Chips on Surface A which are longer or wider than 1/3 of the distance between the outer diameter and the inner pocket are unacceptable. If a chip in the notch covers more than half the width of the notch, then the part is unacceptable. | 3 each surface, 5 total |
| Figure 1 Nominal OD of less than 1.00in. (25.4mm) | B | Chips on Surface B which are longer than 1/3 of the height of the part (C dimension) or 2mm whichever is greater are unacceptable. | 3 each surface, 5 total |
| Figure 1 Nominal OD of greater than or equal to 1.00in. (25.4mm) | A | Chips on Surface A which are longer or wider than 1/4 of the distance between the outer diameter and the inner pocket are unacceptable. If a chip in the notch covers more than half the width of the notch, then the part is unacceptable. | 3 each surface, 5 total |
| Figure 1 Nominal OD of greater than or equal to 1.00in. (25.4mm) | B | Chips on Surface B which are longer than 1/3 of the height of the part (C dimension) or 2mm whichever is greater are unacceptable. | 3 each surface, 5 total |
| Figure 2 With and without ID | A | Chips on Surface A which are longer or wider than 1/10 of outer diameter to a max of 7mm are unacceptable | 3 each surface, 5 total |
| Figure 2 With and without ID | B | Chips on Surface B which are longer than 1/3 of the height of the part (C dimension) or 2mm whichever is greater are unacceptable. | 3 each surface, 5 total |

2.0      Cracks:

2.1	Parallel to the circumference with cumulative length equal to 1/3 of the relative core circumference. Radiating cracks less than 1/10 of outer diameter, maximum of 1 allowed. No open cracks allowed.

3.0	Ragged Edges:

3.1	Ragged edges which are a series of small chips usually along an edge having a width less than 1mm (0.039in) allowed around entire edge.

- Pits:

4.1	See chip spec.

- Stains and Discolourations:

5.1	Stains and discolourations which do not affect the performance of the part are 	acceptable.

- Pullout:

6.1	No more than 1/4 of the area of any surface can be affected by pullout and must be less than .005” deep. Ground discs shall have no pullout.

7.0	Revision History:

| Revision Number | Reason for Change | Revision Date |
| --- | --- | --- |
| 1 | Added Figure 2 and updated entire document | 3/21/11 |
| 2 | Revised Title | 12/22/23 |

# Text boxes

Surface B

Surface A

Surface B

Surface A

Figure 1

Figure 2

Inner pocket

Notch width