Flat Cable EMI Suppression Cores  (PN Product Classes that could apply:  26, ref: 03,04))

# Type I

# Type II

Split Round Cable Suppression Cores

# Type III                                                            Type IV

# 0.1 Limits for Irregularities: Type I

| Type | Location | Max. Size Allowed | Max Count Allowed |
| --- | --- | --- | --- |
| Cracks | Surface A radiating/lengthwise | 1/3 (33%) wall thickness unopened |  |
|  | Surface B & C radiating/lengthwise | 1/5 (20%) length unopened | 3 per part total |
|  | All Surfaces perpendicular to the length(parallel to flux) | 1/5 (20%) perimeter(surfaces B & C) unopened |  |
| Bumps | All Surfaces | 0.050 in (1.27 mm), affected dimension must be within specification | Unlimited |
| Chips, Pits | Surface A | 1/2 (50%) of wall thickness up to max equiv. area of 5 mm x 7 mm | 3 on each surface, 5 total |
|  | Surface B | 1/5 (20%) length of surface up to max equiv. area of 5 mm x 7 mm |  |
|  | Surface C | 1/5 (20%) length of surface up to max equiv. area of 5 mm x 7 mm |  |
| Crazing | All Surfaces | No limit | N/A |
| Pullout | All Surfaces | 0.005in (0.127mm) deep | Cumulative area of pullout must be less than 25% (1/4) of the relevant surface area |
| Sharp Edges | All Burnished Surfaces | None | Sharp edges not allowed on burnished cores |
|  | All Unburnised Surfaces | N/A | Sharp edges allowed on unburnished cores only |
| Ragged Edges | All Surfaces | 0.020 in (0.508 mm) max. penetration | Unlimited |
| Stains and Discoloration | All Surfaces | No limit if performance of part is not affected | Unlimited |

# 0.2 Limits for Irregularities: Type II

| Type | Location | Max. Size Allowed | Max Count Allowed |
| --- | --- | --- | --- |
| Cracks | Surface A radiating/lengthwise | 1/3 (33%) wall thickness unopened | 3 per part total |
|  | Surface B, C & D radiating/lengthwise | 1/5 (20%) length unopened |  |
|  | Surfaces A, B & C perpendicular to the length(parallel to flux) | 1/5 (20%) outer perimeter(surfaces B & C) unopened |  |
|  | Surface D perpendicular to the length(parallel to flux) | Unopened |  |
| Bumps | Unground surfaces | 0.050 in (1.27 mm), affected dimension must be within specification | Unlimited |
| Chips, Pits | Surface A | 1/2 (50%) of wall thickness up to max equiv. area of 5 mm x 7 mm | 3 on each surface, 5 total |
|  | Surface B | 1/5 (20%) length of surface up to max equiv. area of 5 mm x 7 mm |  |
|  | Surface C | 1/5 (20%) length of surface up to max equiv. area of 5 mm x 7 mm |  |
|  | Surface D | 1/3 (33%) Width of surface up to max equiv. area of 5 mm x 7 mm |  |
| Crazing | All surfaces | No limit | N\A |
| Pullout | All Surfaces | 0.005in (0.127mm) deep | Cumulative area of Pullout must be less than 25% (1/4) of the relevant surface area |
| Sharp Edges | All Burnished Surfaces | None | Sharp edges not allowed on burnished cores |
|  | All Unburnised Surfaces | N/A | Sharp edges allowed on unburnished cores only |
| Ragged Edges | All surfaces | 0.020 in (0.508 mm) max. penetration | Unlimited |
| Stains and Discoloration | All surfaces | No limit if performance of part is not affected | Unlimited |

# 0.3 Limits for Irregularities: Type III & IV

| Type | Location | Max. Size Allowed | Max Count Allowed |
| --- | --- | --- | --- |
| Cracks | Surface A radiating/lengthwise | 1/3 (33%) wall thickness unopened | 3 per part total |
|  | Surface B, C & D radiating/lengthwise | 1/5 (20%) length unopened |  |
|  | Surfaces A, B & C perpendicular to the length(parallel to flux) | 1/3 (33%) outer perimeter(surfaces B & C) unopened |  |
|  | Surface D perpendicular to the length(parallel to flux) | Unopened |  |
| Bumps | Unground surfaces | 0.050 in (1.27 mm), affected dimension must be within specification | Unlimited |
| Chips, Pits | Surface A | 1/2 (50%) of wall thickness up to max equiv. area of 5 mm x 7 mm | 3 on each surface, 5 total |
|  | Surface B | 1/5 (20%) length of surface up to max equiv. area of 5 mm x 7 mm |  |
|  | Surface C | 1/5 (20%) length of surface up to max equiv. area of 5 mm x 7 mm |  |
|  | Surface D | 1/3 (33%) Width of surface up to max equiv. area of 5 mm x 7 mm |  |
| Crazing | All surfaces | No limit | N\A |
| Pullout | All Surfaces | 0.005in (0.127mm) deep | Cumulative area of Pullout must be less than 25% (1/4) of the relevant surface area |
| Sharp Edges | All Burnished Surfaces | None | Sharp edges not allowed on burnished cores |
|  | All Unburnised Surfaces | N/A | Sharp edges allowed on unburnished cores only |
| Ragged Edges | All surfaces | 0.020 in (0.508 mm) max. penetration | Unlimited |
| Stains and Discoloration | All surfaces | No limit if performance of part is not affected | Unlimited |

1.0	Revision History:

| Revision Number | Reason for Change | Revision Date |
| --- | --- | --- |
| 1 | revised section 2.2 added surface drawing D | 10/1/99 |
| 2 | Revised the complete VIC | 4/7/14 |
| 3 | Revised the complete VIC | 1/20/15 |
| 4 | Revised section 0.1 Type 1 Chips, Pits | 12/13/17 |
| 5 | Revised Title | 12/22/23 |

# Text boxes

Surface A

Surface C

Surface B

Surface C

Surface A

Surface B

Surface D

Surface A

Surface D

Surface B

Surface C