0.0	PC Bead – Generic  (PN Product Classes that could apply:  29)

1.0	Chips:

1.1	Chips on Surface B which are longer than 1/8 of the height (C dimension) of the 	part, or are wider than 1/8 of the length (A dimension) of the part, are 	unacceptable.

1.2	Chips on Surface C which are longer than 1/8 of the height (C dimension) of the 	part, or are wider than 1/8 of the width (B dimension) of the part, are 	unacceptable.

1.3	Chips on Surface D which are longer than 1/8 of the length (A dimension) of the 	part, or are wider than 1/4 of the width (B dimension) of the part, are 	unacceptable.

1.4	Parts with more than two chips are unacceptable.

2.0	Cracks:

2.1	Cracks are unacceptable.

2.2	Crazing which does not affect the mechanical or electrical integrity of the part is 	acceptable.

3.0	Ragged Edges:

3.1	Ragged edges on the lip surrounding Surface A which are longer than 1/4 of the 	length of the part or which penetrate the entire thickness of the lip are 	unacceptable.

3.2	Ragged edges on the legs on Surface D of Type II parts which are longer than 1/8 	of the length of the part or which penetrate the entire thickness of the leg are 	unacceptable.

4.0	Stains and Discolorations:

4.1	Stains and discolorations which do not affect the performance of the part are 	acceptable.

5.0	Wire:

5.1	Exposed copper on the wire is unacceptable.

5.2	Wire shavings on assembled beads are unacceptable.

6.0	Pullout:

6.1	Pullout on Surface A or Surface D which does not interfere with the holes in the 	part is acceptable.

7.0	Revision History:

| Revision Number | Reason for Change | Revision Date |
| --- | --- | --- |
| 1 | Revised Title | 12/22/23 |