0.0	Multihole Plates – Generic  (PN Product Classes that could apply:  26, 53)

1.0	Chips:

1.1	Chips which are deeper than .020 inches are unacceptable.

1.2	Chips which penetrate the holes on Surface A are unacceptable.

1.3	Chips which extend more than 1/2 of the way down the corner of a part are 	unacceptable.

1.4	Chips on Surface A which are longer or wider than 1/5 of the width of the part (B 	dimension) are unacceptable.

1.5	Parts with more than two chips are unacceptable.

2.0	Cracks:

2.1	Cracks radiating from the holes on Surface A are unacceptable.

2.2	Cracks which run up and down the C dimension on Surface B or Surface C are 	unacceptable.

2.3	Surface crazing is acceptable.

3.0	Ragged Edges:

3.1	For parts which are shorter than 1.000 inches, ragged edges which penetrate more 	than .010 inches into the part are unacceptable.

3.2	For parts which are not shorter than 1.000 inches, ragged edges which penetrate 	more than .025 inches into the part are unacceptable.

3.3	Ragged edges which penetrate the holes on Surface A are unacceptable.

4.0	Pits and Bumps:

4.1	Pits which do not exceed .025 inches in diameter are acceptable.

4.2	Bumps which do not exceed .010 inches in height are acceptable.

5.0	Stains and Discolorations:

5.1	Stains and discolorations which do not affect the performance of the part are 	acceptable.

6.0	Faced Multihole Plates:

6.1	On faced multihole plates, parts with visibly discernable slants are unacceptable.

6.2	Questionable parts should be referred to the team leader responsible for the part or 	a QC Inspector.

7.0	Pullout:

7.1	Minor to moderate pullout on surfaces to be faced is acceptable.  Parts with major 	or questionable pullout should be referred to a QC Inspector.

8.0	Blocked ID’s

8.1	Blocked ID’s are unacceptable.

9.0	Revision History:

| Revision Number | Reason for Change | Revision Date |
| --- | --- | --- |
| 1 | Tightened spec in 1.4; added 4.2 | 4/1/98 |
| 2 | Removed section 7.2 | 10/12/12 |
| 3 | Added section 8.0 and 8.1 | 6/6/14 |
| 4 | Revised Title | 12/22/23 |