# Rods – General  (PN Product Classes that could apply:  30, 31, 40, 42)

# Refer to the most current revision of the Fair-Rite Products document Visual Inspection – Definitions & General Criteria for irregularity definitions.

Figure 1

Figure 2

Figure 3

# Limits for Chips by Part Size

  - The largest dimension of any chip may never exceed the general maximum set in Visual Inspection – Definitions & General Criteria.

  - Maximum amount of material missing from all chips combined cannot exceed 10% by volume.

Figure 1

| Core Size | Surface | Max Size Allowed | Max Qty |
| --- | --- | --- | --- |
| Nominal OD of less than 3.2mm | A, B | No limit though no broken parts allowed | N/A |
| Nominal OD of 3.2mm to 6.3mm | A | No limit | N/A |
|  | B | Less than 1/3 of the Bead length | 1 |
| Nominal OD greater than 6.3mm to 12.7mm | A | No limit | 3 on each surface, 5 total |
|  | B | Less than 1/4 of the Bead length or 1/2 of the wall thickness, whichever is smaller |  |
| Nominal OD greater than 12.7mm | A | Less than 1/2 of the wall thickness to max of 5 mm | 3 on each surface, 5 total |
|  | B | Less than 1/4 of the Bead length to a max equivalent area of 5mm x 7mm; less than max depth of 0.25mm |  |

Figure 2

| Core Size | Surface | Max Size Allowed | Max Qty |
| --- | --- | --- | --- |
| Nominal OD of less than 6.3mm | A | 1/2 of OD or 1mm, whichever is greater | 2 |
|  | B | OD | 2 |
| Nominal OD of 6.3mm to 12.7mm | A | 3mm | 2 |
|  | B | 1/4 of OD or 1/10 of Length, whichever is smaller up to 5mm | 2 |
| Nominal OD of greater than | A | 1/4 of OD up to 5mm | 2 |
| 12.7mm | B | 1/4 of OD or 1/10 of Length, whichever is smaller | 2 |

- Limits for Cracks

Figure 1

| Crack Type | Max Size Allowed | Max Qty |
| --- | --- | --- |
| Radiating / Lengthwise | 1/5 of Wall Thickness | 1 |
| Parallel to Circumference | 1/3 of Circumference (cumulative) – must be unopened | 1 |

Figure 2

| Crack Type | Max Size Allowed | Max Qty |
| --- | --- | --- |
| Radiating / Lengthwise | None | N/A |
| Parallel to Circumference | 1/3 of Circumference (cumulative) – must be unopened | 1 |

- Limits for Pullout, Bumps, Pits, etc.

| Type | Max Size Allowed | Max Qty |
| --- | --- | --- |
| Crazing | No limit | N/A |
| Pits | Reference Chip criteria | Reference Chip criteria |
| Bumps | Small to moderate Bumps that do not interfere with part’s fit or function | Unlimited |
| Ragged Edges | 1mm | Entire length of relevant edge(s) |
| Pullout | 0.075mm depth | Cumulative area of Pullout must be less than 1/4 of the relevant surface area |
| Sticking | No limit | N/A |

- Limits for Flash

Figure 1

| Core ID Size | Max Size Allowed |
| --- | --- |
| Less than or equal to 3mm | Flash is allowed. However, flash can never interfere with part size. |
| Greater than 3mm | Flash is allowed unless the part is burnished. If the part is burnished, no flash is allowed. Flash can never interfere with part size. |

- Guidelines for Rods less than 0.75mm in diameter:

  - These sized parts which are not visually inspected by automated means are not expected to be defect-free.

  - A packaged quantity of these sized parts can typically contain a defect level of up to 0.5%. An additional quantity of 0.5% above the label quantity will be added to each packaged container to offset this maximum defect level.

- Associated Documents:

  - Fair-Rite Products: Visual Inspection – Definitions & General Criteria

- Revision History:

| Revision Number | Reason for Change | Revision Date |
| --- | --- | --- |
| 1 | Complete revision | 5/6/16 |
| 2 | Added section 1.2 | 9/18/17 |
| 3 | Revised Title | 12/22/23 |

References:

International Electrotechnical Commission (IEC) International Standard 60424-1: Ferrite Cores – Guide on the Limits of Surface Irregularities Part 1: General specification   (First Edition 1999-05)

International Electrotechnical Commission (IEC) International Standard 60424-4: Ferrite Cores – Guide on the Limits of Surface Irregularities Part 4: Ring-cores   (First Edition 2001-02)